## Slide 1: 금속 유동 해석 (Metal Flow Analysis)
Prof. Youngung Jeong (정영웅)
yjeong@changwon.ac.kr
#52208
Department of Metallurgy and Materials Science and Engineering

## Slide 2: Information
No particular textbook
  Reference books
  Recommended readings
Interactions
  I do not know everything
  During lecture
    If things are not clear, blame me
  After lecture
    Email: yjeong@changwon.ac.kr
    Knock knock knock #52208
Notes: 교재설명
수업 진행 방식
질문의 중요성

## Slide 3: Assessment (to be determined)
1/3 Attendance
1/3 Assignment (Quiz)
1/3 Final

## Slide 4: Objectives (overall)
Understand the theories associated with metal plasticity
Understand how material scientists / engineers represent the mechanical behavior in terms of mathematical expressions
Successfully analyze / visualize experimental data / conduct some statistical estimation

## Slide 5: Survey (who’s enrolled?)
Let’s take a moment for me to figure out who’s enrolled
  Understand your background by surveying the past lectures you’ve taken
  Do NOT leave your personal information
(Action required) Please send your email address to me
youngung.jeong@gmail.com
yjeong@changwon.ac.kr

## Slide 6: Lecture 1. Uniaxial tension test

## Slide 7: Objectives
Understand uniaxial tension test
Understand how to describe the behavior of metals subjected to uniaxial loading and the standard engineering quantities that are used in practical applications to characterize the mechanical properties
Understand how to process the draw data collected in a uniaxial tension test to obtain a few material properties

## Slide 8: Uniaxial tension test (일축 인장 실험)
(a) A strip tensile test piece and (b) a round bar specimen.
변형률
변형의 정도
변형이 ‘얼마나’ 되었는가?
변형이 일어나기 전과 후의 차이는?
물성 (material property)를 측정하는 방법?
Examples:
Thermal Conductivity
Thermal expansion coefficient
Stiffness
Notes: Stress is force divided by the area to which it is applied.
Strain is a measure to quantify the amount of ‘deformation’ applied to the tested piece.

## Slide 9: Stress (응력) and strain (변형률)
Stress 와 strain 으로 측정할 수 있는 물성은? (기계적 물성)
Strain 측정법?
  Extensometer?
  Lattice?
  Strain gauge (저항 변화)
  Digital Image Correlation (using contrast between pixels, speckle pattern)
Stress 측정법?
  Load-cell
  Crystal Lattice (Diffraction)

## Slide 10: Elasticity and plasticity
탄성이란?
소성이란?
Can you explain it in the atomic scale?
  (Reminders: Atomic bonding, repulsive and attractive forces)
Can you explain it in the macro scale?

## Slide 11: Typical behavior expected from a mild steel sample
What properties can be extracted from this data?
Strain hardening (work hardening)
Yield stress
Ultimate tensile stress
Total elongation
Elastic modulus
Load is dependent on the size of material. A material property does not scale with the amount of applied load.
What about extension?

## Slide 12: Assignment
Determine Engineering stress/strain curves
Determine True stress/strain curves
The data will be emailed to you after lecture